MDF1 Bending Strength Prediction — Baseline ML Summary (V1)

Objective
Develop a first machine learning baseline to predict labBendingAvg for the MDF1 production line using Ksoft-derived process data and lab-linked observations. The aim is to establish a reliable prediction baseline and identify the main process variables influencing bending strength.

Dataset and Preparation
The raw Ksoft export contained 3,128 rows and 1,165 columns. After schema validation, cleaning, target filtering, and removal of one high-missing feature (operFibresDensity), the usable modeling dataset was reduced to 486 observations. The retained data covers the period from 2025-08-01 to 2026-03-29. In addition to the original process variables, 26 engineered features were created to represent aggregated press-pressure, temperature, and thickness behavior.

Modeling Approach
A time-based split was used to reflect production reality, with 388 rows for training and 98 rows for testing. Both Linear Regression and Random Forest were evaluated. For this baseline, the experiment was intentionally structured to remove operPressSpeed from the selected feature set in order to reduce dependence on a single potential proxy variable and focus on more interpretable process signals.

Baseline Performance
The baseline results for labBendingAvg were:

- Random Forest: MAE 2.93, RMSE 4.46, R² 0.7274

- Linear Regression: MAE 4.08, RMSE 5.53, R² 0.5813

These results confirm that bending strength can be predicted with good accuracy from the available MDF1 process data, and that nonlinear modeling provides a clear improvement over a linear baseline.

Main Process Drivers Identified
The most influential variables in the approved baseline were:

- rawThickness

- thicknessClosed_mean

- pressPressureMid_mean

- pressPressureC_mean

- pressPressureGlobal_mean

- pressPressureGlobal_min

- thicknessClosed_std

- pressPressureR_mean

- thicknessClosed_range

- tempGlobal_mean

This indicates that bending strength is primarily influenced by a combination of board thickness, press-pressure distribution, thickness stability, and overall thermal/process conditions.

Key Interpretation
Compared with density prediction, the bending model shows a stronger role for thickness-related engineered features, while aggregated pressure features remain highly influential. This is physically plausible and suggests that bending performance is tied not only to overall press loading but also to the uniformity and stability of board formation.

Conclusion
The V1 baseline successfully demonstrates that labBendingAvg is learnable from Ksoft-derived MDF1 process data with meaningful accuracy. The resulting model is driven by process-relevant engineered features rather than unstable or overly narrow proxy signals, making it a strong reference baseline for the next modeling phase.

Next Step
Freezing this bending model as the approved baseline, retain the exported feature-importance files for review, and continue the same pipeline for the next target: labEModulAvg.